	[image: image14.png]



	SINERGI Vol. xx, No. x, February 20xx: xxx-xxx http://publikasi.mercubuana.ac.id/index.php/sinergi http://doi.org/10.22441/sinergi.xxxx.x.xxx
	[image: image15.png]s SINERGI

PISSN: 1410-2331 e-ISSN: 2460-1217
VOL. 25, NO. 1, FEBRUARY 2021

‘Accredied SINTA 2 by KEMENRISTEKDIKTI, Decree No: 10E/KPTI2018







	SINERGI Vol. xx, No. x, xxxxxx 20xx: xxx-xxx


	p-ISSN: 1410-2331  e-ISSN: 2460-1217



	Experimental investigation on stability and thermal conductivity of SiO2 nanoparticle as green nanofluids for application thermal system
	[image: image17.wmf]1

211

2

()1

VVVV

f

f

æö

D=-=-

ç÷

èø




Anwar Ilmar Ramadhan1*, Efrizon Umar2, Tri Yuni Hendrawati3, Alvika Meta Sari4, Istianto Budhi Rahardja5
1 Department of Mechanical Engineering, Faculty of Engineering, Universitas Muhammadiyah Jakarta, Indonesia. 

2 National Research and Innovation Agency, Indonesia. 
3 Department of Chemical Engineering, Faculty of Engineering, Universitas Muhammadiyah Jakarta, Indonesia. 
4 Department of Chemical Engineering, Faculty of Engineering, Universitas Muhammadiyah Jakarta, Indonesia. 
5 Department of Mechanical Engineering, Institut Teknologi PLN, Indonesia. 
	Abstract 

In recent years, research has focused on improving the thermo-physical properties of single component nanofluids. Therefore, there has not been much research on green nanofluids. So green nanofluids need to be developed to improve heat transfer performance. Stability and thermal conductivity of Nano-silicate suspended in a base mixture of water /ethylene glycol with ratio 60:40, different volume concentrations were investigated. The experiments carried out were the stability of the green nanofluids investigated for volume concentrations of 0.1~0.3%, and temperature conditions from 30 to 70°C for measurement of thermal conductivity using TEMPOS Thermal Properties Analyzer. The experimental results showed that the stability analysis of the green nanofluids prepared by the UV-Vis method was stable up to 30 days after preparation with a sonication time of 1 hour with a ratio of 70-80%. The evaluation of the zeta potential for green nanofluids obtained a value of 33.57 mV with a moderate stability classification. The highest thermal conductivity for the green nanofluids was obtained at 0.3% and the maximum increase was up to 17% higher than the base liquid (W/EG). Green nanofluids with a concentration of 0.1% gave the lowest effective thermal conductivity of 1.09 time at 70°C.
This is an open access article under the CC BY-SA license
[image: image2.png](<) DO




	Keywords: 

Empty Palm Oil Shell; Green nanofluids; Nano-Silicate, Stability; Thermal conductivity;

Article History:

Received: May 2, 2019

Revised: May 29, 2019

Accepted: June 2, 2019

Published: June 2, 2019

Corresponding Author:

Anwar Ilmar Ramadhan
Department of Mechanical Engineering, Universitas Muhammadiyah Jakarta, Indonesia

Email: anwar.ilmar@umj.ac.id 



INTRODUCTION 
Indonesia is the largest producer of palm oil in the world. Indonesia in 2020 produced 44.8 million tons of palm oil with a total area of palm oil plantations of 14,457 million hectares [1]. In the palm oil processing process, palm oil is produced as the main product and waste is also produced as a by-product. Waste produced in the form of liquid waste and solid waste. Liquid waste occurs in the processing of fresh fruit bunches, while solid waste is the first waste produced from palm oil processing [2].

A material that has high porosity and a large surface area is silica (SiO2). There are many uses for it in pharmaceuticals, fillers and catalysts [3]. To produce SiO2 in an industrial environment, sodium silicate is used, where the smelting of quartz sand and sodium carbonate requires a large amount of energy [4]. Extensive studies have attempted to extract silica from various agricultural waste products such as rice husk, corn and coconut cob ash and palm oil waste [2, 5]. As far as we know, studies on OPEFB (empty palm oil bunches) as a source of silica still need to be explored.

Recently, nano-silica has been used as a fluorophore carrier [5, 6], for the controlled release of drug molecules, as an antiseptic agent [7, 8], and as a biosensor [9]. Different silanol groups in nanosilica can change the crystalline behaviour of the polymer matrix, increase the effect of hydrogen bonding, and change the fluorescence properties. The most important property of polymers is their heat resistance; this affects the spectral stability, mechanical properties, lifetime, and other material properties 
 ADDIN EN.CITE 
[4, 10-13]
.

Nanofluid is a liquid suspension containing metal or non-metal nanoparticles with a special size (1-100 nm) that is dispersed into the base fluid. In 1995, the concept of nanofluids was first introduced by Choi, et al. [14]. This new method is proven to increase heat transfer by increasing the thermo-physical properties of nanofluids. Nanofluids are known for applications in heating and cooling processes. The main cooling process is an important part of industrial applications such as power plants, chemical processes, microelectronics, transportation, and automotive cooling systems 
 ADDIN EN.CITE 
[15-17]
. The influence of solid particles can change the thermal properties of the working fluid. Several researchers have conducted research on thermal conductivity, dynamic viscosity and stability of the produced nanofluid 
 ADDIN EN.CITE 
[18-23]
. Green nanofluids or bio-nanofluids, or environmentally friendly nanofluids derived from several sources from natural materials [24, 25]. Highly colloidal stable green nanofluids as alternative working fluids are essential for their effective use in different thermal systems [26]. Based on previous research, there is very little research on the development of green nanofluids in the world.

Nanofluid preparation methods are important to minimize agglomeration of nanoparticles so as to increase stability. The most common processes used in the manufacture of nanofluids are one-step and two-step methods. The one-step method is the process of synthesizing nanoparticles and simultaneously dispersing them in an alkaline liquid. Another method of nanofluid preparation is known as the two-step method. There are two processes in this method, namely (i) synthesis of nanoparticles in powder form (ii) dispersion of nanoparticles into the base liquid to form a stable and homogeneous solution 
 ADDIN EN.CITE 
[27, 28]
.

The stability of the nanofluid and the size of the nanoclusters affect parameters in thermal conductivity 
 ADDIN EN.CITE 
[21, 29-32]
. Nanofluid stability is defined as the resistance of nanoparticles to aggregation. Factors such as Van der Waals attraction cause aggregation, which results in the formation of nanoclusters contained in nanofluids 
 ADDIN EN.CITE 
[33-35]
. The formation of nanoclusters depends on their size, which causes the sedimentation of particles in the nanofluid. The stability of nanofluids has a significant effect. There are two testing methods, quantitative and qualitative. UV-Vis spectrophotometric measurements have been used to quantitatively characterize the stability of nanoparticles from dispersions [21, 30]. Can be applied to all base fluids, while zeta potential analysis has the limitation of base fluid viscosity [36]. In other literature studies, different techniques are used to stabilize nanoparticles in liquids such as ultra-sonication, additional surfactants, surface modifiers and pH adjustment 
 ADDIN EN.CITE 
[4, 37, 38]
. For qualitative testing by visually seeing the sedimentation from the nanofluid made. The thermal conductivity of nanofluids is highly dependent on the stability of nanoparticles dispersed in the base fluid 
 ADDIN EN.CITE 
[32, 39, 40]
.

Thus many researchers carry out important thermal conductivity investigations in understanding the behavior of nanofluids for further application in heat transfer applications. Thermal conductivity is an important factor affecting heat transfer enhancement 
 ADDIN EN.CITE 
[41-44]
. There are several factors that affect thermal conductivity such as: concentration, temperature, particle size, surface to volume ratio of nanoparticles, and nanofluid stability 
 ADDIN EN.CITE 
[45-48]
. Turgut et al. [49], proved that the thermal conductivity increased by 7.4% with the volume fraction of the particles above the alkaline liquid. Investigation of Al2O3-Cu composite nanofluids with water as the base fluid was carried out by Suresh, et al. [50], they reported an increase of up to 12% with increasing volume concentration.

The stability and thermo-physical properties of various types of green nanofluids are very important to study. This aims to understand the stability and behavior of nanofluids as well as factors that affect properties that can improve heat transfer performance. Based on the information obtained by the author, the study of the influence of nanoparticles on green nanofluids is limited to the literature. Based on these problems, this research was carried out by emphasizing the influence of nanosilicate from empty palm shell (EPS) on the stability and thermal conductivity of green nanofluids.

METHOD

Preparation of green nanofluids
The production of green nanofluids involves mono nanofluids, namely SiO2 nanoparticles or Nano-Silicates that are mixed and dispersed in a base fluid mixed with water/EG (60:40). Nano-Silicate is obtained from Empty Palm Oil Shell (EPS) made using the Ultra-Sonication Method. Nano-Silicate nanoparticle size is 51 nm. Nano-Silicate characteristics are given in Table 1. Table 2 presented information properties of Ethylene Glycol.
Table 1. Properties of SiO2 nanoparticles from Empty Palm Oil Shell

	Properties
	SiO2

	Molecular mass, g mol-1
	60.08

	Average particle diameter, nm
	51

	Density, kg m-3
	2220

	Thermal conductivity, W m-1 K-1
	1.4

	Specific heat, J kg-1 K-1
	745


Table 2. Properties of Ethylene Glycol (EG) [51]
	Properties
	EG

	Vapour pressure, mmHg at 20 °C
	0.08

	Boiling point, °C
	195–198

	Melting point, °C
	-13

	Density, g ml−1 at 25 °C
	1.113


A two-step method is used for the preparation of green nanofluids. Green nanofluid is prepared by mixing Nano-silicate with water/EG mixture, and sonication. The production of green nanofluid begins with the calculation of the required volume according to its concentration. In this research, green nanofluids were made with volume concentrations of 0.1, 0.2, and 0.3%. The nanofluid was first prepared at the highest concentration, 0.3% and then diluted to a lower concentration. Arrangement of green nanofluids based on Figure 1.

[image: image3.png]Magnetic

Base Fluid

Nanoparticles
Suspension

Stirring
——

(EG/Water) T

Nano-Silicate

(SiO, Nanoparticle)

Green
Nanofluids

Ultrasonication
Vibration





Figure 1. The preparation of green nanofluids
SiO2 nanoparticles or Nano-Silicates are available in powder form with a weight concentration of 25% for SiO2. Equation (1) [35, 52] is used to convert from weight concentration to volume concentration. Dilution from a higher volume concentration to a lower volume concentration using Eq. (2) [53] by adding the base fluid (ΔV).

[image: image1.jpg]®

Check for
updates





 

         


(1)

[image: image14.png]
(2)

Nano-Silica is mixed together with a mixture of Water/EG in a ratio of 60:40 to form a green nanofluid. A total volume of 100 mL was prepared for the concentration of green nano liquid. The green nanofluid solution was mixed together using a magnetic stirrer for 15 minutes. The solution then undergoes a sonication process for 1 hour using ultrasonic immersion to increase stability.

Stability of green nanofluids
Investigating the stability of green nanofluid in this research was done through UV-Vis spectrophotometer measurement, visual observation and Zeta potential. UV-Vis was performed for 30 days (720 hours) with varying sonication times. The wavelength of the UV-Vis spectrophotometer is set at 850 nm following the research of Hamid, et al. [54]. UV-Vis measures the absorption and light scattering intensity of the nanofluid by comparing the intensity level with the base fluid. The absorbance ratio of the sonication time is different during the sedimentation time at a constant wavelength (λ) of 850 nm. Stability evaluation with UV-Vis was also used by previous research [55]. Sedimentation with visual observation is done for up to 30 days. Green Nanofluid will be considered stable when its concentration is constant. Previously, the same method to observe the visual sedimentation of nanofluids was prepared by Habibzadeh, et al. [29]. Measurements with zeta potential were performed using a Zetasizer Nano ZS (Malvern Instruments Ltd., GB) [55].

Thermal conductivity measurement of green nanofluids

The thermal conductivity measurement method follows the ASTM D5334 and IEEE 442-1981 standards, using the TEMPOS Thermal Property Analyzer shown in Figure 2. Thermal sample conductivity test section, KS-1 sensor to read k [W/m K], measuring bottle to enter the sample to be tested, and the TEMPOS controller is an important part of the thermal conductivity measuring device. The TEMPOS Thermal Property Analyzer instrument uses a transient line heat source to measure thermal properties. Thermal conductivity measurements were performed for temperatures varying from 30 to 70 °C. A water bath is used to keep the sample temperature constant. Previously, the thermal conductivity value from the thermal conductivity sensor was validated using liquid glycerine standards supplied by Meter Group. The measured K is 0.286 W/m K with an accuracy of ± 0.35%. The measurement of thermal conductivity was done several times and the average was taken, the measurement time was 15 minutes for each set of data at different temperatures. This is important to minimize the occurrence of errors in measurements with free convection due to temperature variations along the sensor that is in direct contact with the liquid sample.
[image: image4.jpg]Nanofluids

Water sample
bath -

TEMPOS




Figure 2.
TEMPOS Thermal Properties Analyzer to the measurement of thermal conductivity

RESULTS AND DISCUSSION

Stability of green nanofluids

Observations of the absorbance for volume concentrations of 0.1, 0.2 and 0.3% are shown in Figure 3. The absorbance of green nanofluid increases linearly with increasing volume concentration. This trend is in accordance with the Beer-Lambert Law, namely the absorbance value is equal to the concentration. The stability of the green nanofluid was further confirmed by the absorbance ratio, Ar and presented in Figure 4. 
The absorbance ratio at 0.1% volume concentration of green nanofluid for 4 different sonication variations. The ideal absorbance ratio is one (100%) indicating ideal fluid stability. Condition variations with 3 hours of sonication began to decrease after 50 hours by 70% and continued to decrease until it stabilized at 30 days (720 hours) by 50%. While the sonication time is 2 hours, it remains at a good concentration ratio value of about 70~80% up to 30 days later. The condition of sonication time for 1 hour, reduced the absorbance ratio by 60%. For variations of sonication 0 hours or after preparation there was a decrease of 40%.
 
[image: image5.wmf]0.0

0.1

0.2

0.3

0.4

0.5

1.0

1.5

2.0

2.5

3.0

 

 

  Volume Concentration 

µ�0

 0.1 Green Nanofluids

 0.2 Green Nanofluids

 0.3 Green Nanofluids

Absorbance, A

Concentration, 

µ


Figure 3. UV-Vis spectrophotometer linear relation graph between absorbance and green nanofluids concentration

[image: image6.wmf]0

200

400

600

800

1000

1200

0.0

0.2

0.4

0.6

0.8

1.0

 

 

Absorbance ratio, 

A

r

 (

�

�

��

�

)

Sedimentation time, 

t

 (hour)

Sonication time 

     (hour)

 0.0

 1.0

 2.0

 3.0


Figure 4. The absorbance ratio of green nanofluids for different sonication time within 30 day

From the figure it can be seen that the sonication time of 2 hours shows the best absorbance ratio compared to other sonication times. Thus, the manufacture of green nanofluid in this study used 2 hours for the sonication process. The absorbance ratio finding was obtained 70-80% for 30 days. The absorbance ratio of the green nanofluid in this study was compared with Hwang, et al. [56] and shown in Figure 5. 
Investigations by Hwang, et al. [56], used multi-wall carbon nanotubes (MWCNT) in an aqueous base fluid. As shown in the graph, MWCNT nanofluid has poor stability. In this study, Nano-Silicate was used in the EG/Water mixed base liquid and used a sonication time of 2 hours. The absorbance ratio finding was obtained 70-80% for 30 days. This condition is stable.


[image: image7.wmf]0

50

100

150

200

250

0.2

0.4

0.6

0.8

1.0

1.2

1.4

                                            Type Nanofluid                  

�

��4u

    

 Present 

                  Green Nanofluids               0.1

    

 

 Hwang et al            MWCNT/DI Water             1.0

    

 

 

Absorbance ratio, 

A

r

 (

�

�

��

�

)

Sedimentation time, 

t 

(hour)

Figure 5. Comparison of absorbance ratio with sedimentation ratio from literature

Zeta potential measurement is one of the most critical tests to validate the stability quality of nanofluids through electrophoretic behavior studies 
 ADDIN EN.CITE 
[36, 57]
. Zeta potential evaluation is the standard quantitative method for stability evaluation [21, 34]. Usually, the accepted zeta potential values are summarized on Table 3. Generally, suspensions with a measured zeta potential above 30 mV (absolute value) are considered to have good stability [57]. The absolute value of the zeta potential was used to show the agglomeration of SiO2 nanoparticles in EG/W. The higher the absolute value, the better the dispersion of the particles, was resulting in better stability.
Table 3. Zeta potential and classification stability [57]
	Zeta potential (mV)
	Stability

	0
	Little or no stability

	15
	Some stability 

	30
	Moderate stability

	45
	Good stability

	60
	Very good stability


Measurement of zeta potential for nanofluid green recorded up to 33.57 mV. The results were then compared with the stability classification of nanofluids based on zeta potential with moderate stability values compiled by Ghadimi, et al. [57] as shown in Figure 6. An absolute value above 30 mV is desired for good stability of the green nanofluid. It is proven that the green nanofluid is beyond the stable limit of 30 mV. Therefore, the evaluation of zeta potential has confirmed the stability of green nanofluid.


[image: image8.wmf]0

10

20

30

40

50

60

70

 

Very good 

stability

Good 

stability

Moderate 

stability

Some 

stability 

 

 

Zeta Potential (mV)

 Present 

 Ghadimi et al (2011)


Figure 6. Zeta potential of green nanofluids

Figure 7 shows an image of the green-W/EG nanofluid for a volume concentration of 0.1. 0.2, and 0.3%. Green Nanofluids-W/EG images were taken only after preparation and after 30 days. Base on Figure 7a–c, no particle sedimentation was observed after the nanofluid was prepared after 21 days. Agglomeration appears in the 30-day sample in Figure 7 d.

[image: image9.png](c) 21 days
(d) 30 days




Figure 7. Sedimentation observation of green nanofluids: (a) 0 day, (b) 7 days, (c) 21 days, and (d) 30 days
Validation of thermal conductivity with ASHRAE

Thermal conductivity measurements using the TEMPOS Thermal Properties Analyzer are presented in Figure 8. Thermal conductivity measurement data needs to be validated by comparing with ASHRAE [58] for EG/Water (60:40). The deviation for the measured data is less than 1.0% compared to ASHRAE [43]. Reddy et al. [59] conducted a validation test for deviation from the base fluid of up to 2.5% compared to ASHRAE [58]. Therefore, further measurements and investigations for the thermal conductivity of the green nanofluids were carried out.

[image: image10.wmf]20

30

40

50

60

70

80

0.38

0.40

0.42

0.44

0.46

0.48

0.50

 

 

 EG/W (Base Fluid)

 ASHRAE (2009)

Thermal conductivity, 

k

 [W/m.K]

Temperature, 

T

 [

o

C]


Figure 8. Validation of EG/Water (40:60) with ASHRAE for thermal conductivity

The thermal conductivity of green nanofluids

The relationship between the thermal conductivity of green nanofluid and temperature for volume concentrations of 0.1~0.3% is shown in Figure 9. The thermal conductivity of green nanofluid for variations in volume concentration can increase in relation to temperature and is higher than the base liquid. Furthermore, the highest thermal conductivity was obtained for a volume concentration of 0.3%. While the volume concentration of 0.1% gives the lowest thermal conductivity among the temperatures studied. In this study, the effect of the SiO2 nanoparticle size of 50 nm on the increase in thermal conductivity. So it has a strong bond in filling the empty space. To increase the contact area for intermolecular conduction, resulting in a higher rate of heat transfer during collisions with Brownian motion [60]. The effective thermal conductivity of the green nanofluid is presented in Figure 10. The results show that the effective thermal conductivity increases with a volume concentration of 0.3% in the green nanofluid, except for 0.1% volume where the effective thermal conductivity of the nanofluid is lowest. The effective thermal conductivity in green nanofluids can significantly influence the relationship between volume concentration and each temperature series.


[image: image11.emf]20 30 40 50 60 70 80

0.36

0.40

0.44

0.48

0.52

0.56

0.60

 EG/W

 ASHRAE 

 

 

Thermal conductivity, 

k

 [W/m.k]

Temperature, T [

o

C]

  Concentration [%]

 0.1

 0.2

 0.3


Figure 9. The experimental thermal conductivity of green nanofluids


[image: image12.wmf]20

30

40

50

60

70

80

1.00

1.05

1.10

1.15

1.20

1.25

1.30

1.35

 

 

Effective thermal conductivity [

k

eff

=k

nf

/k

bf

]

Temperature, 

T

 [

o

C]

  Concentration [%]

 0.1

 0.2

 0.3


Figure 10. The effective thermal conductivity of green nanofluids

Comparison of thermal conductivity with literature 
Figure 11 shows a comparison of the effective thermal conductivity from this study with that of Murshed, et al. [61]. In this study, the effective thermal conductivity of green nanofluid increased 1.08-1.17 times compared to base fluid for a concentration of 0.1%. Murshed, et al. [61], using Al2O3 nanoparticles with a volume concentration of 0.5% of the basic fluid used was a mixture of EG-Water. They proved that the experimental values of different thermal conductivities of nanofluids increased significantly with liquid temperature. This is due to the high fluid temperature increasing the movement of the Brownian nanoparticles. The effect of intense Brownian motion increases the contribution of microconnectivity to heat transfer, so that the thermal conductivity of the nanofluid increases. 

[image: image13.wmf]20

30

40

50

60

70

80

90

0.6

0.8

1.0

1.2

1.4

1.6

 

 

Effective thermal conductivity, 

k

eff

Temperature, 

T

 [

o

C]

                                   Type of nanofluids      

�

 [%]

 Present                Green Nanofluids       0.1

 Murshed et al      Al

2

O

3 

                          0.5


Figure 11. Comparison of green nanofluids of thermal conductivity with the data from literature

CONCLUSION

In this research, the stability of green nanofluid was investigated for a volume concentration of 0.1~0.3%, and temperature conditions from 30 to 70°C for thermal conductivity measurement. The experimental results show that the stability analysis of the green nanofluid made with the UV-Vis method is stable up to 30 days after preparation with a sonication time of 1 hour. A comparison of data on the ratio of concentration to sedimentation for green nanofluid shows that it remains stable with a value of 70-80%. The zeta potential evaluation performed for green nanofluid obtained a value of 33.57 mV with a medium stability classification. Sedimentation from this visual observation is influenced by the gravitational force of the movement of particles that fall in the tube after 30 days. All methods prove that green nanofluids contain SiO2 nanoparticles or nano-silicates. The concentration volume of 0.3% obtained the best according to the effective thermal conductivity compared to 0.1~0.2%.

ACKNOWLEDGMENT

The authors would like to thank the Universitas Muhammadiyah Jakarta, special to the National Research and Innovation Agency of the Republic of Indonesia and LPDP for providing funding and support for this research through the National Research Priority (PRN) with Research and Innovation for Advanced Indonesia (RIIM) in 2024.

REFERENCES
[1]
Y. Sudiyanti, "Pemanfaatan Limbah Biomassa Industri Kelapa Sawit untuk Produksi Bioetanol Generasi 2 dan Co-Products," Lembaga Ilmu Penelitian Indonesia,” Jakarta, 2013.

[2]
P. Velmurugan et al., "Extraction, characterization, and catalytic potential of amorphous silica from corn cobs by sol-gel method," Journal of industrial and engineering chemistry, vol. 29, pp. 298-303, 2015.

[3]
M. F. Anuar, Y. W. Fen, M. H. M. Zaid, K. A. Matori, and R. E. M. Khaidir, "Synthesis and structural properties of coconut husk as potential silica source," Results in Physics, vol. 11, pp. 1-4, 2018.

[4]
I. Kazemi, M. Sefid, and M. Afrand, "A novel comparative experimental study on rheological behavior of mono & hybrid nanofluids concerned graphene and silica nano-powders: Characterization, stability and viscosity measurements," Powder Technology, vol. 366, pp. 216-229, 2020.

[5]
S. Sinyoung, K. Kunchariyakun, S. Asavapisit, and K. J. MacKenzie, "Synthesis of belite cement from nano-silica extracted from two rice husk ashes," Journal of Environmental Management, vol. 190, pp. 53-60, 2017.

[6]
N. Ngadi and N. S. Lani, "Extraction and characterization of cellulose from empty fruit bunch (EFB) fiber," Jurnal Teknologi, vol. 68, no. 5, 2014.

[7]
F. Aulia and S. Marpongahtun, "Studi penyediaan nanokristal selulosa dari tandan kosong sawit (TKS)," Jurnal Saintia Kimia, vol. 1, no. 2, pp. 1-5, 2013.

[8]
K. R. Ningtyas and M. Muslihudin, "Sintesis nanoselulosa dari limbah hasil pertanian dengan menggunakan variasi konsentrasi asam," Jurnal Penelitian Pertanian Terapan, vol. 20, no. 2, pp. 142-147, 2020.

[9]
H. Julianto, M. Farid, and A. Rasyida, "Ekstraksi nanoselulosa dengan metode hidrolisis asam sebagai penguat komposit absorpsi suara," Jurnal Teknik ITS, vol. 6, no. 2, pp. F243-F246, 2017.

[10]
H. Ow, D. R. Larson, M. Srivastava, B. A. Baird, W. W. Webb, and U. Wiesner, "Bright and stable core− shell fluorescent silica nanoparticles," Nano letters, vol. 5, no. 1, pp. 113-117, 2005.

[11]
W. Li, J. Yue, and S. Liu, "Preparation of nanocrystalline cellulose via ultrasound and its reinforcement capability for poly (vinyl alcohol) composites," Ultrasonics sonochemistry, vol. 19, no. 3, pp. 479-485, 2012.

[12]
J. Li et al., "Homogeneous isolation of nanocellulose from sugarcane bagasse by high pressure homogenization," Carbohydrate polymers, vol. 90, no. 4, pp. 1609-1613, 2012.

[13]
M. R. N. Monton, E. M. Forsberg, and J. D. Brennan, "Tailoring sol–gel-derived silica materials for optical biosensing," Chemistry of Materials, vol. 24, no. 5, pp. 796-811, 2012.

[14]
U. S. Choi, "Enhancing Thermal Conductivity of Fluids With Nanoparticles," in Developments and Applications of Non-Newtonian Flows, vol. FED-vol. 231/MD-Vol. 66, D. A. Siginer and H. P. Wang, Eds. New York: American Society of Mechanical Engineers (ASME), 1995, pp. 99–105.

[15]
R. Saidur, K. Leong, and H. Mohammad, "A review on applications and challenges of nanofluids," Renewable and sustainable energy reviews, vol. 15, no. 3, pp. 1646-1668, 2011.

[16]
N. A. Che Sidik, M. N. A. Witri Mohd Yazid, and R. Mamat, "Recent advancement of nanofluids in engine cooling system," Renewable and Sustainable Energy Reviews, vol. 75, pp. 137-144, 2017/08/01/ 2017.

[17]
A. Kasaeian, A. T. Eshghi, and M. Sameti, "A review on the applications of nanofluids in solar energy systems," Renewable and Sustainable Energy Reviews, vol. 43, no. Supplement C, pp. 584-598, 2015/03/01/ 2015.

[18]
W. H. Azmi, K. Abdul Hamid, R. Mamat, K. V. Sharma, and M. S. Mohamad, "Effects of working temperature on thermo-physical properties and forced convection heat transfer of TiO2 nanofluids in water – Ethylene glycol mixture," Applied Thermal Engineering, vol. 106, pp. 1190-1199, 2016.

[19]
M. Gupta, V. Singh, S. Kumar, S. Kumar, N. Dilbaghi, and Z. Said, "Up to date review on the synthesis and thermophysical properties of hybrid nanofluids," Journal of Cleaner Production, vol. 190, pp. 169-192, 2018/07/20/ 2018.

[20]
A. M. Hussein, R. A. Bakar, K. Kadirgama, and K. V. Sharma, "Experimental measurement of nanofluids thermal properties," International Journal of Automotive and Mechanical Engineering, vol. 7, pp. 850-863, 2013.

[21]
R. Choudhary, D. Khurana, A. Kumar, and S. Subudhi, "Stability analysis of Al2O3/water nanofluids," Journal of Experimental Nanoscience, vol. 12, no. 1, pp. 140-151, 2017.

[22]
Y.-j. Hwang et al., "Stability and thermal conductivity characteristics of nanofluids," Thermochimica Acta, vol. 455, no. 1-2, pp. 70-74, 2007.

[23]
G. Yıldız, Ü. Ağbulut, and A. E. Gürel, "A review of stability, thermophysical properties and impact of using nanofluids on the performance of refrigeration systems," International Journal of Refrigeration, vol. 129, pp. 342-364, 2021.

[24]
R. G. Saratale et al., "New insights on the green synthesis of metallic nanoparticles using plant and waste biomaterials: current knowledge, their agricultural and environmental applications," Environmental Science and Pollution Research, vol. 25, pp. 10164-10183, 2018.

[25]
K. Wickramasinghe, H. Sasahara, E. Abd Rahim, and G. Perera, "Green Metalworking Fluids for sustainable machining applications: A review," Journal of Cleaner Production, vol. 257, p. 120552, 2020.

[26]
L. H. Kumar, S. Kazi, H. Masjuki, and M. Zubir, "A review of recent advances in green nanofluids and their application in thermal systems," Chemical Engineering Journal, vol. 429, p. 132321, 2022.

[27]
N. A. Che Sidik, M. Mahmud Jamil, W. M. A. Aziz Japar, and I. Muhammad Adamu, "A review on preparation methods, stability and applications of hybrid nanofluids," Renewable and Sustainable Energy Reviews, vol. 80, pp. 1112-1122, 2017/12/01/ 2017.

[28]
W. Yu and H. Xie, "A review on nanofluids: preparation, stability mechanisms, and applications," Journal of Nanomaterials, vol. 2012, p. 1, 2012.

[29]
S. Habibzadeh, A. Kazemi-Beydokhti, A. A. Khodadadi, Y. Mortazavi, S. Omanovic, and M. Shariat-Niassar, "Stability and thermal conductivity of nanofluids of tin dioxide synthesized via microwave-induced combustion route," Chemical Engineering Journal, vol. 156, no. 2, pp. 471-478, 2010.

[30]
S. M. Abbasi, A. Rashidi, A. Nemati, and K. Arzani, "The effect of functionalisation method on the stability and the thermal conductivity of nanofluid hybrids of carbon nanotubes/gamma alumina," Ceramics International, vol. 39, no. 4, pp. 3885-3891, 2013.

[31]
R. Agarwal, K. Verma, N. K. Agrawal, R. K. Duchaniya, and R. Singh, "Synthesis, characterization, thermal conductivity and sensitivity of CuO nanofluids," Applied Thermal Engineering, vol. 102, no. Supplement C, pp. 1024-1036, 2016/06/05/ 2016.

[32]
M. Batmunkh et al., "Thermal conductivity of TiO2 nanoparticles based aqueous nanofluids with an addition of a modified silver particle," Industrial & Engineering Chemistry Research, vol. 53, no. 20, pp. 8445-8451, 2014.

[33]
Babita, S. K. Sharma, and S. M. Gupta, "Preparation and evaluation of stable nanofluids for heat transfer application: A review," Experimental Thermal and Fluid Science, vol. 79, no. Supplement C, pp. 202-212, 2016/12/01/ 2016.

[34]
S. U. Ilyas, R. Pendyala, and N. Marneni, "Stability of nanofluids," in Engineering Applications of Nanotechnology: Springer, 2017, pp. 1-31.

[35]
H. Setia, R. Gupta, and R. Wanchoo, "Stability of nanofluids," in Materials Science Forum, 2013, vol. 757, pp. 139-149: Trans Tech Publ.

[36]
I. M. Mahbubul, R. Saidur, M. A. Amalina, E. B. Elcioglu, and T. Okutucu-Ozyurt, "Effective ultrasonication process for better colloidal dispersion of nanofluid," Ultrasonics Sonochemistry, vol. 26, no. 0, pp. 361-369, 2015.

[37]
R. S. Kumar and T. Sharma, "Stability and rheological properties of nanofluids stabilized by SiO2 nanoparticles and SiO2-TiO2 nanocomposites for oilfield applications," Colloids and Surfaces A: Physicochemical and Engineering Aspects, vol. 539, pp. 171-183, 2018/02/20/ 2018.

[38]
Y. Rao, "Nanofluids: stability, phase diagram, rheology and applications," Particuology, vol. 8, no. 6, pp. 549-555, 2010.

[39]
B. Barbés et al., "Thermal conductivity and specific heat capacity measurements of Al2O3 nanofluids," Journal of Thermal Analysis and Calorimetry, journal article vol. 111, no. 2, pp. 1615-1625, February 01 2013.

[40]
H. Chiam, W. Azmi, N. Usri, R. Mamat, and N. Adam, "Thermal conductivity and viscosity of Al2O3 nanofluids for different based ratio of water and ethylene glycol mixture," Experimental Thermal and Fluid Science, vol. 81, pp. 420-429, 2017.

[41]
T. T. Baby and S. Ramaprabhu, "Experimental investigation of the thermal transport properties of a carbon nanohybrid dispersed nanofluid," Nanoscale, vol. 3, no. 5, pp. 2208-14, May 2011.

[42]
Z. Said, M. H. Sajid, M. A. Alim, R. Saidur, and N. A. Rahim, "Experimental investigation of the thermophysical properties of AL2O3-nanofluid and its effect on a flat plate solar collector," International Communications in Heat and Mass Transfer, vol. 48, no. 0, pp. 99-107, 2013.

[43]
S. F. A. Talib et al., "Thermophysical Properties of Silicon Dioxide (SiO2) in Ethylene Glycol/Water Mixture for Proton Exchange Membrane Fuel Cell Cooling Application," Energy Procedia, vol. 79, no. Supplement C, pp. 366-371, 2015/11/01/ 2015.

[44]
A. Yasinskiy et al., "Dramatically enhanced thermal properties for TiO2-based nanofluids for being used as heat transfer fluids in concentrating solar power plants," Renewable Energy, vol. 119, pp. 809-819, 2018/04/01/ 2018.

[45]
S. Mousavi, F. Esmaeilzadeh, and X. Wang, "Effects of temperature and particles volume concentration on the thermophysical properties and the rheological behavior of CuO/MgO/TiO 2 aqueous ternary hybrid nanofluid: Experimental investigation," Journal of Thermal Analysis and Calorimetry, vol. 137, pp. 879-901, 2019.

[46]
D. Sui, V. H. Langåker, and Z. Yu, "Investigation of thermophysical properties of nanofluids for application in geothermal energy," Energy Procedia, vol. 105, pp. 5055-5060, 2017/05/01/ 2017.

[47]
S. Suresh, K. P. Venkitaraj, P. Selvakumar, and M. Chandrasekar, "Synthesis of Al2O3–Cu/water hybrid nanofluids using two step method and its thermo physical properties," Colloids Surfaces A, vol. 388, no. 1–3, pp. 41-48, 2011.

[48]
W. Yu, H. Xie, Y. Li, L. Chen, and Q. Wang, "Experimental investigation on the thermal transport properties of ethylene glycol based nanofluids containing low volume concentration diamond nanoparticles," Colloids and Surfaces A: Physicochemical and Engineering Aspects, vol. 380, no. 1-3, pp. 1-5, 2011.

[49]
A. Turgut, I. Tavman, M. Chirtoc, H. P. Schuchmann, C. Sauter, and S. Tavman, "Thermal conductivity and viscosity measurements of water-based TiO2 nanofluids," International Journal of Thermophysics, vol. 30, no. 4, pp. 1213-1226, 2009.

[50]
S. Suresh, K. Venkitaraj, P. Selvakumar, and M. Chandrasekar, "Effect of Al2O3–Cu/water hybrid nanofluid in heat transfer," Experimental Thermal and Fluid Science, vol. 38, pp. 54-60, 2012.

[51]
A. Ahmadi Nadooshan, "An experimental correlation approach for predicting thermal conductivity of water-EG based nanofluids of zinc oxide," Physica E: Low-dimensional Systems and Nanostructures, vol. 87, pp. 15-19, 2017/03/01/ 2017.

[52]
A. I. Ramadhan, W. H. Azmi, R. Mamat, K. A. Hamid, and S. Norsakinah, "Investigation on stability of tri-hybrid nanofluids in water-ethylene glycol mixture," in IOP Conference Series: Materials Science and Engineering, 2019, vol. 469, no. 1, p. 012068: IOP Publishing.

[53]
W. H. Azmi, K. Abdul Hamid, N. A. Usri, R. Mamat, and M. S. Mohamad, "Heat transfer and friction factor of water and ethylene glycol mixture based TiO2 and Al2O3 nanofluids under turbulent flow," International Communications in Heat and Mass Transfer, vol. 76, pp. 24-32, 2016.

[54]
K. A. Hamid, W. Azmi, M. Nabil, R. Mamat, and K. Sharma, "Experimental investigation of thermal conductivity and dynamic viscosity on nanoparticle mixture ratios of TiO2-SiO2 nanofluids," International Journal of Heat and Mass Transfer, vol. 116, pp. 1143-1152, 2018.

[55]
M. A. Fikri, W. M. Faizal, H. K. Adli, Z. Bo, X. X. Jiang, and A. I. Ramadhan, "Investigation on stability of TiO2-SiO2 nanofluids with ratio (70: 30) in W/EG mixture (60: 40)," in IOP Conference Series: Materials Science and Engineering, 2021, vol. 1062, no. 1, p. 012020: IOP Publishing.

[56]
Y. Hwang et al., "Stability and thermal conductivity characteristics of nanofluids," Thermochimica Acta, vol. 455, no. 1-2, pp. 70-74, 2007.

[57]
A. Ghadimi, R. Saidur, and H. Metselaar, "A review of nanofluid stability properties and characterization in stationary conditions," International Journal of Heat and Mass Transfer, vol. 54, no. 17-18, pp. 4051-4068, 2011.

[58]
ASHRAE Handbook - Fundamentals (SI Edition). Atlanta: American Society of Heating, Refrigerating and Air-Conditioning Engineers, Inc., 2009.

[59]
M. C. S. Reddy and V. V. Rao, "Experimental studies on thermal conductivity of blends of ethylene glycol-water-based TiO2 nanofluids," International Communications in Heat and Mass Transfer, vol. 46, no. 0, pp. 31-36, 2013.

[60]
Z. Aparna, M. M. Michael, S. K. Pabi, and S. Ghosh, "Diversity in thermal conductivity of aqueous Al2O3- and Ag-nanofluids measured by transient hot-wire and laser flash methods," Experimental Thermal and Fluid Science, vol. 94, pp. 231-245, 2018/06/01/ 2018.

[61]
S. Murshed, K. Leong, and C. Yang, "Investigations of thermal conductivity and viscosity of nanofluids," International journal of thermal sciences, vol. 47, no. 5, pp. 560-568, 2008.




	A. Adriansyah et al., Author Template for SINERGI 
	1


	2
	A. Adriansyah et al., Author Template for SINERGI


	A. Adriansyah et al., Author Template for SINERGI
	3



[image: image15.png][image: image16.wmf]1

100100

w

wp

wr

f

ww

rr

=

æö

+-

ç÷

èø

_1744790931.bin

_1744825869.bin

_1744826227.bin

_1745310315.bin

_1744807475.bin

_1744788287.bin

_1744788861.bin

_1744785296.bin

