SINERGI

Response to the Comments of Reviewers

Title: Investigation on mechanical properties and microstructural characteristic of rice hush ash based geopolymer mortar as patch repair

Response to the Comments of Reviewer A:

| Comments | Response |
| --- | --- |
| - Revised title to: _Investigation of mechanical properties and microstructural characteristics of rice hush ash-based geopolymer mortar as patch repair. | Thank you for your suggestion. The title has been changed to be Investigation of mechanical properties and microstructural characteristics of rice hush ash-based geopolymer mortar as patch repair. (Please see p. 1, Title) |
| - The introduction is thorough but somewhat lengthy. It could be condensed to focus more on the key points relevant to the study. | Thank you very much for the review. The introduction has been changed as the suggestion (Please see p. 1, Section Introduction) |
| - If the material being tested does not meet the standards, does it have to be restarted from the start? Or is it enough to prepare new material? | It is enough just to prepare the new material. The Figure 1 has been changed. (Please see Figure 1) |
| - Check the composition of the geopolymer mortar mixture again. Table 1 shows the different volumetric weights of each composition variation, and the ratio of RHA to activator does not match the explanation given. | The composition used has a fine aggregate to binder ratio of 70%:30%, while the binder materials consist of 3 variations with ratios of 60%:40%, 55%:45%, and 50%:50%. Additionally, alkali activators NaOH and Na2SiO3 are used in a 1:3.5 ratio with a molarity of 14 M (NaOH 14M). The amount of water used is 25% of the binder weight. The text has been modified. |
| - SNI is not ASTM; please choose which one to use! | The authors choose the ASTM, the text has been modified. |
| - Please use the latest version | SNI 03-2847-2019, the text has been modified. |
| - Please mention the number of standards completely and added in references | The standard has been written completely. |
| - Please cite references related to the explanation given. | The new references have been added. |
| - State the data sources used and add references. | The data source and the reference has been added. |
| - Authors should add statement about novelty and some comparisons with similar works to highlight the contribution. | The statement about the novelty has been included in the last paragraph of the discussion. Thank you very much for your suggestion and review. |